|  |  |  |  |
| --- | --- | --- | --- |
| **BITUMEN CSS-1h** | | | |
| **Property** | **Min** | **Max** | **Test Method** |
| **Viscosity, Say bolt Furol at 25°C,SFS** | **20** | **100** | **ASTM D244** |
| **Storage stability Test, 24-h, %** | **-** | **1** | **ASTM D6930** |
| **Particle Charge Test** | **Positive** | | **ASTM D244** |
| **Sieve Test, %** | **-** | **0.1** | **ASTM D6933** |
| **Cement Mixing Test,%** | **-** | **2.0** | **ASTM 6935** |
| **Distillation** | | | |
| **Residue %** | **59** | **-** | **ASTM D244** |
| **Test On Residue From Distillation** | | | |
| **Penetration, 25°C(77°F), 100g, 5s** | **40** | **90** | **ASTM D5** |
| Y:\LOGO RDR\RDR Logo Vertical.png**Ductility, 25°C(77°F), 5 cm/min, cm** | **40** | **-** | **ASTM D113** |
| **Solubility in trichloroethylene, %** | **97.5** | **-** | **ASTM D2042** |