|  |  |  |
| --- | --- | --- |
| Heavy Slack Wax | | |
| Characteristic | **Test Method** | **Value** |
| Kinematic Viscosity @ 100 oC ˚C | **ASTM D445** | **6 – 7.5** |
| Oil Content (%wt) | **ASTM D721** | **7 – 11** |
| Melting Point | **ASTM D87** | **56 – 65** |
| Color | **ASTM D1500** | **1.5** |