|  |  |  |  |
| --- | --- | --- | --- |
| **BITUMEN K160** | | | |
| **Property** | **Min** | **Max** | **Test Method** |
| **Viscosity, Say bolt Furol at 50°C,SFS** | **20** | **100** | **ASTM D244** |
| **Storage stability test, 24-h, %** | **-** | **1** | **ASTM D6930** |
| **Demulsibility, 35 ml, 8% Dioctyl sodium sulfosuccinate, %** | **40** | **-** | **ASTM D6936** |
| **Particle Charge Test** | **Positive** | | **ASTM D244** |
| **Sieve Test, %** | **-** | **0.1** | **ASTM D6933** |
| **Distillation** | | | |
| **Solvents, By Volume Of Emulsion %** | **-** | **3** | **ASTM D6997** |
| **Residue %** | **60** | **-** | **ASTM D244** |
| **Test On Residue From Distillation** | | | |
| **Penetration, 25°C(77°F), 100g, 5s** | **100** | **250** | **ASTM D5** |
| **Ductility, 25°C(77°F), 5 cm/min, cm** | **40** | **-** | **ASTM D113** |
| **Solubility in trichloroethylene, %** | **97.5** | **-** | **ASTM D2042** |