|  |
| --- |
| RPO (Rubber Process Oil) |
| Characteristic | **Test Method** | **Value** |
| **Heavy** | **Light** |
| Kinematic Viscosity @ 100 oC (cSt) | **ASTM D445** | **35 min** | **35 max** |
| Density @ 15  oC | **ASTM D1298** | **1.050** | **1.010** |
| Flash Point ( oC) | **ASTM D93** | **200-230** | **200-230** |
| RI @ 70  oC | **ASTM D1218** | **1.56** | **1.55** |