|  |  |  |
| --- | --- | --- |
| BITUMEN MC 30 | | |
| ****Characteristic**** | **Value** | **Test Method** |
| Kinematic Viscosity at 60°C (cSt) | **30-60** | **ASTM D-2170** |
| Flash Point (top open cup)(°C) | **38 min** | **ASTM D-3143** |
| Distillate, %volume of total distillate to at 360°C:  To 225°C  To 260°C  To 316°C | **25 max**  **40-70**  **75-93** | **ASTM D-402** |
| Residue from Distillation to 360°C (%Vol by difference) | **50 min** |
| ****Test on Residue from Distillation**** | | |
| Viscosity at 60°C | **30-120** | **ASTM D-2170** |
| Penetration at 25°C (dmm) | **120-250** | **ASTM D-5** |
| Ductility at 25°C (cm) | **100 min** | **ASTM D-113** |
| Solubility in Trichloroethylene (%wt) | **99 min** | **ASTM D-2042** |
| Water Content (%vol) | **0.2 max** | **ASTM D-95** |