|  |
| --- |
| BITUMEN MC 70 |
| ****Characteristic**** | **Value** | **Test Method** |
| Kinematic Viscosity@ 60°C (cSt) | **70-140** | **ASTM D-2170** |
| Flash Point (Top open cup)$ $(°C) | **38 min** | **ASTM D-3143** |
| Distillate, %volume of total distillate to @ 360°C:to 225°Cto 260°Cto 316°C | **20 max****20-60****65-90** | **ASTM D-402** |
| Residue from Distillation to 360°C (%Vol by difference) | **55 min** | **ASTM D-402** |
| Test on Residue from Distillation |
| Viscosity@ 60°C (cSt) | **30-120** | **ASTM D-2170** |
| Penetration @ 25°C (dmm) | **120-250** | **ASTM D-5** |
| Ductility @ 25°C (cm) | **100 min** | **ASTM D-113** |
| Solubility in Trichloroethylene (%wt) | **99 min** | **ASTM D-2042** |
| Water Content (%vol) | **0.2 max** | **ASTM D-95** |