|  |
| --- |
| **Semi Refined-Paraffin Wax 1.5% Max Oil Content** |
| **Characterization** | **Test Method** | **Value** |
| Color | - | White |
| Oil Content | ASTM D721 | 1.5% Max |
| RI (at 70°C ) | ASTM D1218 | 1.44210 |
| Melting Point | ASTM D87 | 60 - 66°C |
| Flash Point | ASTM D 93-13 | 250°C |
| Kinematic Viscosity @100°C ;cst | ASTM D445 | 6.5 - 7 |
| Odour | - | Odourless without smell |