|  |  |  |
| --- | --- | --- |
| Residue Wax (Foots Oil) | | |
| Characteristic | **Test Method** | **Value** |
| Kinematic Viscosity @ 100 oC (mm2/s) | **ASTM D445** | **5.5-7.5** |
| Density @ 15.6  oC (kg/m3) | **ASTM D4052** | **830-870** |
| Flash Point ( oC) | **ASTM D92** | **Min 220** |
| Color | **ASTM D1500** | **Max 5** |
| Oil Content (%wt) | **ASTM D721** | **25-50** |