|  |
| --- |
| **Fully Refined-Paraffin Wax 0.5-1% Oil Content** |
| **Characterization** | **Test Method** | **Value** |
| Color (Lovibond) | Method (2” cell) | White/Transparent |
| Oil Content  | ASTM D721 | 0.5-1% wt |
| Melting Point  | ASTM D127 | 58-62°C |
| Flash Point | ASTM D 92 | Min 300°C |
| Kinematic Viscosity at 100°C  | ASTM D445 | 5-6 CST |