|  |  |  |
| --- | --- | --- |
| **Semi Refined-Paraffin Wax 1-3% Oil Content** | | |
| **Characterization** | **Test Method** | **Value** |
| Color | ASTM D1500 | <0.5 |
| Oil Content | ASTM D721 | 1-3% |
| Specific Gravity @ 15 °C | ASTM D 2726 | 0.85 |
| Melting Point | ASTM D87 - 09 | 66-68ᵒC |
| Kinematic Viscosity @100°C ;cst | ASTM D445 | 5.5-6.5 Cst |