|  |
| --- |
| **Semi Refined-Paraffin Wax 2-4% Oil Content** |
| **Characterization** | **Test Method** | **Value** |
| Color  | ASTM D1500 | White |
| Congealing Point  | ASTM D938 | 58-60°C |
| Oil Content  | ASTM D721 | 2-4% |
| Specific Gravity @ 15 °C | ASTM D 2726 | 0.80 |
| Melting Point  | ASTM D127 | 60-63°C |
| Flash Point | ASTM D 92 | Min 190 |
| Kinematic Viscosity @100°C ;Cst | ASTM D445 | 4.0-6.0 |