|  |
| --- |
| **Semi Refined-Paraffin Wax 5-7% Oil Content** |
| **Characterization** | **Test Method** | **Value** |
| Color  | ASTM D1500 | Yellowish white |
| Oil Content  | ASTM D721 | 5-7% |
| Melting Point  | ASTM D87 | 62-65°C |
| Flash Point | ASTM D 93-13 | 220-240 |
| Kinematic Viscosity @100°C ;Cst | ASTM D445 | 6.0-7.5 |