|  |  |  |
| --- | --- | --- |
| Base Oil SN500 (High VI) | | |
| Characteristic | **Test Method** | **Value** |
| Appearance | **Visual** | **C & B** |
| Color | **ASTM D-1500** | **Max 1** |
| Viscosity @ 100 oC, CSt | **ASTM D-445** | **Min 10.5-11.2** |
| Viscosity Index; Min | **ASTM D-2270** | **Min 90** |
| Flash Point, (Min)  oC | **ASTM D-92** | **Min 245** |
| Pour Point, (Max)  oC | **ASTM D-97** | **Max 6** |