|  |
| --- |
| Base Oil SN600 (Low VI) |
| Characteristic | **Test Method** | **Value** |
| Appearance | **Visual** | **C & B** |
| Color  | **ASTM D-1500** | **Max 3** |
| Viscosity @ 100 oC, CSt | **ASTM D-445** | **Min 12.6** |
| Viscosity Index; Min | **ASTM D-2270** | **Min 80** |
| Flash Point, (Min)  oC | **ASTM D-92** | **Min 235** |
| Pour Point, (Max)  oC  | **ASTM D-97** | **Max 3** |