|  |  |
| --- | --- |
| Formed Sulfur | |
| Analysis & Methods  (Latest issue of test methods used; unless, otherwise stated) | **Result** |
| Average Samples | Limited |
| Ash Content (PPM) | Max 200 |
| Solubility in Water | Insoluble |
| Moisture Content (PPM) | Max 850 |
| Acidity (AS H2SO4) (PPM) | Max 50 |
| Purity (On Dry Basis) (PPM) | Min 99.8 |
| Appearance | Yellow, Granule |
| Bulk Density | Min 1000 Kg/m3 |
| Size of Distribution (Approx.) | 3-6 mm |