|  |
| --- |
| Formed Sulfur |
| Analysis & Methods(Latest issue of test methods used; unless, otherwise stated)  | **Result** |
| Average Samples | Limited  |
| Ash Content (PPM) | Max 200 |
| Solubility in Water  | Insoluble  |
| Moisture Content (PPM) | Max 850 |
| Acidity (AS H2SO4) (PPM) | Max 50 |
| Purity (On Dry Basis) (PPM) | Min 99.8 |
| Appearance  | Yellow, Granule  |
| Bulk Density  | Min 1000 Kg/m3 |
| Size of Distribution (Approx.)  | 3-6 mm |